GEO 2003 Blades: Assessing the specification of the manufactured parts.

# Overview

On the 19th December 2002, we received the latest set of GEO blades, as designed by Mike Plissi here at the IGR. The blades were made by Accrofab (Derby) the same company has manufactured all previous GEO blades.

We received the following:

- 2 x Trapezoidal blade design				440g load to deflect flat

- 18 x Conventional/Traditional blade design		440g load to deflect flat

# Aims and Objectives

- To check the maximum deflection of each blade against the value specified in the Manufacturing drawings

- To check the thickness of each blade against the value specified in the Manufacturing drawings

- To check the deflection of each blade under a load of 440g (the value at which each blade should be ‘flat’)

- To find out what load is required to make each blade flat, should any blade not meet up to the specification

1.0 Comparing the measured Maximum Deflection with the specified

The measured values were significantly lower than those specified in Engineering Drawings as the graph above demonstrates. The pink line represents the 42.8mm deflection specified in the drawings of the conventional blade. The blue points mark the measured values, which are on average 3.8mm below what is demanded.

The trapezoidal blades suffered a similar fate.

2.0 Checking the thickness

The mean value of measured blade thickness was 0.9452mm over all (18 + 2) blades.

The thickness specified in the manufacturing drawing was 1mm. This significant difference is illustrated above.

3.0 Under a 440g Load

As may be expected from blades that, when inspected, have thickness and max. deflection values that are less than were specified, all blades deflect too much. On average, 12.56mm below the horizontal.

4.0 Load to make each Blade flat

The mean of the masses required to deflect each of the blades into a flat position is 329g. (I.e. 111g less than was desired)

# Conclusions

Mike Plissi will be contacting the company to give them feedback on this set of blades.

The fact is that they do not meet the desired specification, which is an unsatisfactory result.

Possible questions to ask are:

* What were the exact processes involved in the manufacture? (How long did each take? What are the possible shortcomings of each process?)

* Was this chain of events consistent with those previously employed to make these blades?

If there were differences, what are the reasons for these differences?

* To what degree were the blades inspected after manufacture?

Why is the blade thickness over 0.05mm out? (How can this be remedied? How tight a tolerance can be specified on such dimensions?)

Why was the radius of curvature not accurate? How can this be remedied?

END.